## Slide 1: Improving the coherence time of superconducting qubits by design
A procedure to calculate participation ratios
Notes: In my search to increase the coherence time of transmon qubits I have focused on one specific source of decoherence. Namely the two-level systems in lossy layers.

## Slide 2: Sources of decoherence
A prominent source of decoherence are two-level states (TLS) on various surfaces.
Layers containing a high concentration of TLSs are created during production of the qubit.
These are the “lossy-layers”.
Notes: These layers containing two-level systems are a prominent source of decoherence, if not a limiting factor to the coherence time of qubits.

## Slide 3: Lossy layers
3 lossy-layers are considered:
Metal-Vacuum interface (MV)
Metal-Substrate interface (MS)
Substrate-Vacuum (SV)
Notes: I my simulations I have considered three different lossy layers. They are created during different production steps and therefore have a different composition.

## Slide 4: Lossy layers

## Slide 5: Lossy layers

## Slide 6: Lossy layers
Lossy layers have a relatively small thickness of ~3nm
High density of TLSs inducing significant dissipation of energy
Notes: Although the lossy layers are considered to have a relatively small thickness of 3nm compared to the thickness of the pads of 100nm it is the high density of two-level systems the that make the dissipation of energy significant in these layers.

## Slide 7: Lossy layers
Dielectric constants
Metal-Vacuum: Nb-oxides
Metal-Substrate: Si-nitride
Substrate-Vacuum: Si-oxide

## Slide 8: Model of the system
To calculate the energy stored in the lossy layers the E-field in these layers must be know.

## Slide 9: Model of the system
Assumption:
Because the lossy layers on interfaces are very thin, E-field does not change over its thickness.
Notes: Because the lossy layers are so thin compared to the rest of the system it would be undoable to consider them during the simulation in CST. Therefore the assumption is made that the lossy layers do not change the electric field.

## Slide 10: Model of the system
Assumption:
Because the lossy layers on interfaces are very thin, E-field does not change over its thickness.
Fields in green are determined during simulation
Notes: Having made this assumption for the simulation of the qubit it is still necessary to consider the difference in dielectric constants. The amplitude of the field inside the areas containing lossy material is changed accordingly.

## Slide 11: Model of the system
Stored energy:
Notes: https://farside.ph.utexas.edu/teaching/jk1/lectures/node112.html
https://books.google.nl/books?id=mll47bVO29gC&pg=PA1415&lpg=PA1415&dq=tangential+electric+field+superconductor+high+frequency&source=bl&ots=CdOO-SKSTM&sig=WD6728zQIlr839oagMkSicv-3ps&hl=en&sa=X&ved=0ahUKEwiHlOG34YLNAhWKKcAKHbGSDBAQ6AEIKTAB#v=onepage&q=tangential%20electric%20field%20superconductor%20high%20frequency&f=false

## Slide 12: Model of the system
Being able to calculate , it is possible to determine the influence certain design parameters (pad separation, corner radius) and/or changing overall qubit design (interdigitated, padded) on participation ratio.

## Slide 13: Simulation

## Slide 14: Simulation - Setup
Josephson-Junction substituted by an inductance
Notes: E = h*v
hbar = h/2pi

## Slide 15: Simulation - Setup
Josephson-Junction substituted by an inductance

## Slide 16: Simulation - Setup
Pads

## Slide 17: Simulation - Setup
Ground

## Slide 18: Simulation - Setup
Parametrized

## Slide 19: Simulation - Meshing
The initial mesh is a critical factor in reducing simulation time and improving results.
Create fine mesh only at important surfaces
Eliminate Low Quality Mesh Elements
Keep the total amount of mesh elements as low as possible.

## Slide 20: Simulation - Meshing
Divide pads in (several) segments
Adjust maximum mesh size for each segment. Segments closer to edges receive lower maximum.
This creates a fine mesh without adding unnecessary mesh elements.

## Slide 21: Simulation - Meshing
Creating a fine mesh near the edge of the pad simultaneously eliminates most low quality mesh elements.

## Slide 22: Simulation - Meshing

## Slide 23: Simulation - Meshing

## Slide 24: Simulation - Meshing

## Slide 25: Simulation - Meshing

## Slide 26: Simulation - Meshing

## Slide 27: Simulation - Meshing
Simulating the ground plate as a thin sheet eliminates the need for very fine meshing in this area.
Edges of the ground sheet are provide minimal storage of energy compared to pad edges.

## Slide 28: Simulation - Meshing

## Slide 29: Simulation - Meshing

## Slide 30: Post Processing
Export E-field data on different components (ground, substrate, pads) separately.

## Slide 31: Post Processing
Separate data belonging to different lossy layers.
Separate normal and tangential component on SV-interface.
Evaluate given integral (summation in this case)

## Slide 32: First Result - Ratio
IBM E-energy (MV) = 1.2299e-05 J E-energy (MS) = 1.9563e-04 J E-energy (SV) = 6.1201e-05 J p (MV) = 0.0457 p (MS) = 0.7269 p (SV) = 0.2274 | Yale E-energy (MV) = 6.4322e-05 J E-energy (MS) = 2.8180e-04 J E-energy (SV) = 1.4012e-04 J p (MV) = 0.1323 p (MS) = 0.5795 p (SV) = 0.2882

## Slide 33: More pictures

## Slide 34: More pictures

## Slide 35: More pictures

## Slide 36: More pictures

## Slide 37: More pictures